| Product name | Imitated discharge paste |
| --- | --- |
| State | Paste |
| Packing | 20KG/drum |
| Storage | 6 months in cool place |
| Application | Suitable for knitting |
| Features | 1. High fastness 2. High softness 3. SGS detecting passed, no PVC, no heavy metal, no NPEOs. |
| Mix proportion | Imitated discharge paste + pigment (max 12%) |
| Printing process | - Mixing imitated discharge paste, pigment and stirring them evenly. - Printing for 2-3 times (3-4 scrapes per time) - Dry in room temperature for about 24-48 hours ,or baking for 1-3 minutes under 150℃ |
| Attentions |  |
| 品名 | 针织仿拔印浆 |
| 外观 | 乳白色糊状 |
| 包装 | 20KG/桶 |
| 贮存期 | 常温下6个月 |
| 应用 | 针织布 |
| 卖点 | - 易于应用 可使用传统的涂料印花方式，印花处方组分数量少，色浆制备简单，适合大批量生产 - 牢度 耐摩擦和磨损，水洗和干洗牢度好 - 色泽深度和鲜艳度 相似涂料印花效果 - 节省涂料色种用量、手感更加柔软 - 符合美国ASTM对邻苯二甲酸脂和欧盟EN71 Part 3对重金属含量的要求 |
| 调配比例 | 仿拔印浆+ 水性色浆（不超过12%） |
| 工艺流程 | 1. 丝网选用80-100目，用丝印硬方刀75度刮印2-3次。 2. 24-48小时自然干燥，或150度烘烤1-3分钟 |
| 注意事项 |  |